Product name: Aron Alpha Type 401X, 402X, 403X

400X Series

Heat and Impact resistant, metal bonding grade

The Aron Alpha 400X series are modified ethyl 2-cyanoacrylate adhesives. They give a strong bond to metal surfaces, and are more heat and impact resistant with metal than other Cyanoacrylate adhesives.  These characteristics make these adhesives suitable for metal bonding application.

If you have any questions, we are always available to help you. Thank you for your continued business.

Application Examples:

1.	All industries

- Metal bonding with heat, impact, vibration:		Metal

2.	Other

- Heat, impact, vibration:				Metal, Ceramic

- Temporarily bonding, heat, impact, vibration:	Glass

Features:

- Good bonding strength to various materials (especially metal)

- Good tensile shear strength under heated conditions or after heating

- High impact strength

Physical Properties of Aron Alpha 400X Series

|  |  | 401X | 402X | 403X |
| --- | --- | --- | --- | --- |
| Liquid State (before curing) | Appearance | Colorless, Transparent |  |  |
|  | Main Ingredient | Ethyl 2-cyanoacrylate |  |  |
|  | Viscosity (cps, 77˚F) | 2 | 85 | 1500 |
|  | Specific Gravity (d20) | 1.05 |  |  |
|  | Boiling Point (˚C/˚F, 5 mmHg) | About 60/140 |  |  |
|  | Surface Tension (dynes/cm) | 34 |  |  |
|  | Flash Point (˚C/˚F, closed type) | 83/181 |  |  |
|  | Freezing Point (˚C/˚F) | -30/-22 |  |  |
|  | Solubility Parameter | 10-11 |  |  |

|  |  | 401X | 402X | 403X |
| --- | --- | --- | --- | --- |
| Solid State (after curing) | Appearance | Colorless, Transparent |  |  |
|  | Specific Gravity (d20) | 1.25 |  |  |
|  | Refractive Index (n20) | 1.49 |  |  |
|  | Hardness (Rockwell M) | 85 |  |  |
|  | Rate of Line Expansion (x 10-4) | 1.1 |  |  |
|  | Glass Transition Point (˚C/˚F) | 140/284 |  |  |
|  | Dielectric Constant (10MC, 50˚F) | 3.5 |  |  |
|  | Volume dielectric resistivity (Ω-cm, 86˚F) | 1014 |  |  |
|  | Solvent | Acetone, Dimethyl formamide, Dimethyl sulfoxide |  |  |

Setting Times (in seconds for various materials)

| ### Material | Setting Time (sec) |  |  |
| --- | --- | --- | --- |
|  | 401X | 402X | 403X |
| Steel | 15 | 30 | 60 |
| Aluminum | 15 | 60 | 120 |
| Copper | 3 | 5 | 5 |
| Stainless Steel | 15 | 30 | 60 |
| Rigid PVC/Steel | 15 | 30 | 60 |
| Copper/Phenolic resin | 5 | 10 | 30 |
| Aluminum/ABS | 15 | 60 | 120 |
| Stainless Steel/Neoprene | 15 | 60 | 120 |

Bonding Strengths (Tensile measured in psi for various materials)

| #### Material | Tensile Strength (psi) |  |  |
| --- | --- | --- | --- |
|  | 401X | 402X | 403X |
| Steel | 5800 |  |  |
| Aluminum | 5800 |  |  |
| Copper | 5800 |  |  |
| Stainless Steel | 6400 |  |  |
| Rigid PVC/Steel | 2800 |  |  |
| Copper/Phenolic resin | 4300 |  |  |
| Aluminum/ABS | 2600 |  |  |
| Stainless Steel/Neoprene | 360* |  |  |

*Material Failure

Bonding Strengths (Shear measured in psi for various materials)

| #### Material | Shear Strength (psi) |  |  |
| --- | --- | --- | --- |
|  | 401X | 402X | 403X |
| Steel | 3300 |  |  |
| Aluminum | 2500 |  |  |
| Copper | 2800 |  |  |
| Stainless Steel | 3100 |  |  |
| Rigid PVC/Steel | 1000* |  |  |
| Copper/Phenolic resin | 1000* |  |  |
| Aluminum/ABS | 710* |  |  |
| Stainless Steel/Neoprene | 70* |  |  |

* Material Failure

Impact Strength (kgf cm/cm2)

| Material | 401X | 402X | 403X |
| --- | --- | --- | --- |
| Steel | 28 |  |  |
| Aluminum | 13 |  |  |
| Copper | 15 |  |  |
| Stainless Steel | 13 |  |  |
| Brass | 13 |  |  |

Heat Resistance (psi)

- Measured under heated conditions

| Temperature (˚F) x hours | 401X | 402X | 403X |
| --- | --- | --- | --- |
| 212 x 6 | 2800 |  |  |
| 212 x 12 | 2800 |  |  |
| 266 x 6 | 1400 |  |  |
| 266 x 12 | 1400 |  |  |
| 302 x 6 | 570 |  |  |
| 302 x 12 | 430 |  |  |

- Measured at room temperature after cooling

| Temperature (˚F) x hours | 401X | 402X | 403X |
| --- | --- | --- | --- |
| 212 x 6 | 3300 |  |  |
| 212 x 12 | 3300 |  |  |
| 266 x 6 | 2700 |  |  |
| 266 x 12 | 2600 |  |  |
| 302 x 6 | 1800 |  |  |
| 302 x 12 | 1600 |  |  |

Testing Details and Conditions for Testing

## Test Pieces’ measurements

Tensile strength:	0.5 x 0.5 x 1.5 inch; bonded area 0.25 sq. inch

Tensile shear strength:

for plastic and rubber	0.1 x 1.0 x 4.0 inch; bonded area 0.5 sq. inch
for metal		0.064 x 1.0 x 4.0 inch; bonded area 0.5 sq. inch

Bonding atmosphere:	72-75F (22-24˚C), 58-62% relative humidity

Testing Methods:		ASTM D2095, D3164, and D1002

REGULATION

Military Specification – Mill-A-46050C Type II Class varies

Medical assembly - US Plastics Class VI

HOW TO APPLY ARON ALPHA

Clean the surfaces to be bonded and then apply Aron Alpha.  Be sure to apply Aron Alpha to only one of the surfaces to be bonded, preferably the smaller surface, the surface on which the Aron Alpha set time is longer, or the surface looking upward.

A common error in applying Aron Alpha is to apply an excessive quantity of Aron Alpha or to apply too small of a quantity of Aron Alpha in a wide thin film.  In the former case, it is waste of Aron Alpha as well as damaging to the appearance of the bonded materials.  This may also bring about chlorosis or solvent cracks.  In the latter case, the Aron Alpha monomer may harden before the actual bonding starts and this will reduce the bond strength to a great extent.  This is particularly the case with rubber materials.

Therefore, make sure that the nozzle of the Aron Alpha container is touching the surface to be bonded so that you can apply an optimum quantity of Aron Alpha from the container.  Immediately after that, mate the two surfaces and let the Aron Alpha monomer spread between the two surfaces.  It is not necessary to spread the monomer by using a rubbing motion.

Aron Alpha monomer, if kept in the form of a mound on the surface, does not harden for 5 to 10 minutes and retains sufficient bond strength.

OPTIMIUM QUANTITY OF ARON ALPHA

With Aron Alpha bonding, the thinner the film of the Aron Alpha monomer on the surface to be bonded, the greater is the resulting bond strength.  An excessive quantity of Aron Alpha never helps increase the bond strength.  On the contrary, it may bring about chlorosis, solvent cracks, or erosion by the Aron Alpha monomer of the surface to be bonded.

On the other hand, a too scarce quantity of Aron Alpha will also produce unsatisfactory bond strength, hence defective products.  Test results indicate that with Aron Alpha the optimum quantity to be applied at one time is 0.004 - 0.006 g/cm2 or 0.03 - 0.05 mm in terms of film thickness.  On the basis of the value of 5 mg/cm2, you can obtain standard bond strengths as shown in the tables above.

The optimum quantity applied can also be a measure of production control at your plant.  That is, from the predetermined bond area of the material to be bonded, you can figure out in advance how many products or parts can be bonded with, for example, an Aron Alpha 20 gram bottle.  With the figure thus obtained, you can maintain a quantified control of Aron Alpha bonding operation, minimizing the bonding cost and eliminating defective end products.

STORAGE

Conditions to consider when storing Aron Alpha

Humidity

Avoid moist, humid storage conditions.

Fasten cap tightly to avoid exposure to moisture.

Store with desiccant.

Temperature

Avoid storing at a high temperature.

When storing Aron Alpha for an extended period, refrigerate between 40F and 50F.

Sunlight

Avoid direct exposure to ultraviolet light (keep in light-proof packaging).

Other

Never store Aron Alpha with an accelerator.

WARNING

Eye and Skin irritant.  Bonds skin instantly.  Combustible – keep away from heat and flames.  Please read adhesive MSDS before using.

Disclaimer:

Please be advised that test results are those which were prepare at Borden’s laboratory.  The results may vary under actual application conditions.