Product name: Aron Alpha 903TX

Features

Excellent resistance to heat and humidity after bonding various rubbers.

Physical Properties

|  |  | 903TX |
| --- | --- | --- |
| Liquid State (before curing) | Appearance | Colorless and Transparent |
|  | Main Ingredient | Ethyl 2-cyanoacrylate |
|  | Viscosity(cps, 77˚F) | 850 |
| Solid State (after curing) | Appearance | Colorless and Transparent |
|  | Hardness (Shore D, 77°F) | 80 |
|  | Glass Transition Point (˚C/˚F) | 118/245 |

PERFORMANCE

Setting time (sec), bond strength in tension and shear (psi); note:* indicates material failure.

Setting time

| Material | Setting times (sec) |
| --- | --- |
| Rigid PVC | 5 |
| ABS | 10 |
| Natural Rubber | 30 |
| Neoprene Rubber | 5 |
| Copper | 10 |

Bonding strength Tension

| Material | Tensile strengths (psi) |
| --- | --- |
| Rigid PVC | 2400 |
| Aluminum | 1800 |

Bonding strength Shear

| Material | Tensile strengths (psi) |
| --- | --- |
| Natural Rubber | 110* |
| Neoprene Rubber | 110* |

Environmental Resistance

Aged at some conditions and tested @72-75°F (22-24°C),

| Condition | Peel strengths (kgf/inch) |
| --- | --- |
| Initial 72-75°F (22-24°C) | 850 |
| 212°F (100°C) 96hours | 730 |
| -40°F (-40°C) 96hours | 740 |
| 122°F (50°C),95%RH 96hours | 850 |
| -40°F (-40°C)/1hour, 176°F (80°C)/1hour, 84 cycles | 700 |

Material: Butyl Rubber/Steel

Test conditions—Test specimen

Tensile strength: 	0.5 x 0.5 x 1.5 inch; bonded area 0.25 sq. inch

Tensile shear strength:	0.1 x 1.0 x 2.0 inch; bonded area 0.5 sq. inch

Peel strength: 	0.1 x 1.0 x 4-10 inch; bonded area 3 sq. inch

Bonding atmosphere:	72-75F, 58-62% relative humidity

Test Methods:	ASTM D2095, D3164, D1002

HOW TO APPLY ARON ALPHA

Clean the surfaces to be bonded and then apply Aron Alpha.  Be sure to apply Aron Alpha to only one of the surfaces to be bonded, preferably the smaller surface, the surface on which the Aron Alpha set time is longer, or the surface looking upward.

A common error in applying Aron Alpha is to apply an excessive quantity of Aron Alpha or to apply too small of a quantity of Aron Alpha in a wide thin film.  In the former case, it is waste of Aron Alpha as well as damaging to the appearance of the bonded materials.  This may also bring about chlorosis or solvent cracks.

In the latter case, the Aron Alpha monomer may harden before the actual bonding starts and this will reduce the bond strength to a great extent.  This is particularly the case with rubber materials.

Therefore, make sure that the nozzle of the Aron Alpha container is touching the surface to be bonded so that you can apply an optimum quantity of Aron Alpha from the container.  Immediately after that, mate the two surfaces and let the Aron Alpha monomer spread between the two surfaces.  It is not necessary to spread the monomer by using a rubbing motion.

Aron Alpha monomer, if kept in the form of a mound on the surface, does not harden for 5 to 10 minutes and retains sufficient bond strength.

OPTIMIUM QUANTITY OF ARON ALPHA

With Aron Alpha bonding, the thinner the film of the Aron Alpha monomer on the surface to be bonded, the greater is the resulting bond strength.  An excessive quantity of Aron Alpha never helps increase the bond strength.  On the contrary, it may bring about chlorosis, solvent cracks, or erosion by the Aron Alpha monomer of the surface to be bonded.  On the basis of the value of 5 mg/cm2, you can obtain standard bond strengths as shown in the tables above.

STORAGE

Conditions to consider when storing Aron Alpha

Humidity

Avoid moist, humid storage conditions.

Fasten cap tightly to avoid exposure to moisture.

Store with desiccant.

Temperature

Avoid storing at a high temperature.

When storing Aron Alpha for an extended period, refrigerate between 40F and 50F.

Sunlight

Avoid direct exposure to ultraviolet light (keep in light-proof packaging).

Other

Never store Aron Alpha with an accelerator.

WARNING

Eye and Skin irritant.  Bonds skin instantly.  Combustible – keep away from heat and flames.  Please read adhesive MSDS before using.

Disclaimer

Please be advised that test results are those which were prepare at Toagosei America’s laboratory.  The results may vary under actual application conditions.